Reacción del tejido conectivo de ratas a   implantes de tubos de silicona

obturados con un sellador a base de resina ADSEAL (Meta)

AUTORES:

Bideigorri Marcela *,  Salaverry Graciela,  Mandalunis Patricia,  Canzani Jorge.

RESUMEN:

En este estudio “ in vivo” se evaluó la respuesta del tejido subcutáneo de ratas, producida por un sellador endodóntico a base de resinas, el ADSEAL de la firma META (Corea) y su comparación con AH 26(resina epóxica)de la firma Denstply –Maillefer EEUU. Se utilizaron 40 ratas Wistar provistas por el bioterio de la Facultad de Farmacia y Bioquímica de la UBA que fueron divididas en lotes de 10 animales cada uno. En cada animal se colocó tres implantes sobre la espina dorsal, un tubo conteniendo el sellador ADSEAL ,el segundo con AH 26 y el tercer tubo de silicona vacío, para el  control negativo. A intervalos de  7, 14,  30 y 60  días, los animales fueron sacrificados y las muestras extraídas fijadas en formol al 10%. Posteriormente, en la cátedra de Histología y Embriología de la Facultad de Odontología de la U.B.A., las muestras fueron  incluidas en parafina, se realizaron los cortes orientados bajo lupa estereoscópica y posterior tinción. Las reacciones del tejido celular subcutáneo fueron  analizadas histológicamente bajo microscopía óptica de forma cualitativa y cuantitativa.

La biocompatibilidad del material fue interpretada de acuerdo a criterios de la Federación Dental Internacional 1980. Los  resultados fueron analizados estadísticamente con KRUSKAL_WALLIS test.

REFERENCIAS  BIBLIOGRAFÍCAS

1. Park S., Lim S. Cytotoxicity and antibacterial property of a New resin-based sealer.

J Endod 2002; 28:262.PR35

2. Lee J, Kim Y, Bae K.Biocompatibility of two newly-developed resin-based root canal sealers. J Endod 2002;28:263 PR37

3. Tagger M, Tagger E. Subcutaneous  reactions to implantation of tubes with AH26 and Grossman sealer. Oral Surg. Oral Med. Oral Pathol. 1986; 62: 434-40.

4. Reid RJ, Wilson DF, Chau KK, Heithersay GS, Heijkoop PS. Tissue responses to Hydron, assessed by intraosseous implantation. Int Endod J. 1992 Jul;25(4):192-8.

5. Kaplan A, Ormaechea MF, Picca M,  Canzobre MC, Ubios MA. Rheological  Properties and biocompatibility of endodontic sealers. I Endod J.2003;36(8):527-32

6. Zmener O. Tissue response to a new methacrylate-based root canal sealer: preliminary observations in the subcutaneous connective tissue of rats. J Endod 2004; 30(5): 348-351

7. Fonzi L, Gasparoni A, Capezzuoli L, Carboncini S, Belli M, Kaitsas V.In vitro and In vivo biocompatibility tests of some endodontic cements .G Ital Endod.1991;5 (3):70-8

8.Molloy D,Goldman M,White RR,Kabani S. Comparative tissue tolerance of a new endodontic sealer.

Oral Surg Oral Med Oral Pathol 1992;73(4):490-3

9.Zmener O, Gugliemotti MB, Cabrini RL. Quantitative method for the study of biocompatibility of endodontic materials in the rat.  RAOA 1988 Marz;76 (1):27-34

10. Recommenden Standard Practices. Federation Dentaire Internacional, Comisión on dental Materials, Instruments, Equipment and Therapeutics. 1978; vol 30:185-8.