Respuesta del tejido periapical de ratas al endo-cpm sealer

Canzani Jorge H, Salaverry Graciela, Adaro Carolina,

Bua Marcela*, Bideigorry Marcela, Mandalunis Patricia

Carrera de Especialización en Endodoncia USAL/AOA

Cátedra de Histología y Fisiología de la FOUBA

Bioterio Central de la Facultad de Farmacia y Bioquímica UBA

Resumen

Objetivos:El propósito de este estudio fue comparar  histológicamente ,en forma cualitativa y cuantitativa , la respuesta inflamatoria del periodonto ,producida por  un nuevo sellador endodóntico el Endo-CPM sealer (de la firma  EGEO-Argentina ) a base de cemento Portland   con el cemento de Grossman a base de óxido de zinc-eugenol. (Tedekim).

Materiales y métodos :la técnica de Eráusquin /Muruzábal con ciertas modificaciones fue empleada para tal fin.Se utilizaron 80 conductos mesiales de primeros molares inferiores de ratas que fueron divididos en dos grupos, A y B, para ser  obturados con ambos materiales. A intervalos de 14 y 30 días ,los animales fueron sacrificados ,las mandíbulas resecadas ,fijadas en formol al 10 % y descalcificadas para realizar los cortes orientados que posteriormente fueron coloreados con hematoxilina-eosina.

La reacción producida en los tejidos por los selladores ,se evaluó histológicamente bajo microscopia  óptica .

Los resultados están siendo procesados.Hasta el momento resultados preliminares.

Bibliografía:

1.Rickert UG,Dixon CM. J AMER Dent Assoc 1938;25:178

2.Endodontic Practice Lea y Febiger. Philadelphia _USA

3.Eráusquin, J.;Muruzábal M.;(1967): A method for root canal treatment in the molar of the rat.Oral Surg.Oral Med. Oral Path.24(4):540-6

4.Eráusquin J.;Muruzábal M.;1967:Root canal fillings with zinc oxide-eugenol cement in the rat molar.Oral Surg. Oral Med.Oral Path.24(4):547-558

5.Erausquin J,Muruzabal M.,1968:Tissue reaction to root canal cements in the rat molar Oral Surg.Oral Med.Oral Path 26(·):360-373

6.Friend L A.,Browne R M. Tissue reactions to same root filling materials implanted of  the bone of rabbits.Archs Oral Biol.1969;14:629-638

7.Jin –Su Kim, Seung –Ho Baek,Kwang-Sihik Bae.In vivo study on biocompatibility of newly Developer calcuim phosphate root canal sealers. J Endod 2004;30(10):708-11

8.Kaplan A., Ormaechea MF,Pirca M,Canzobre MC,Ubios MA. Rheological         Properties and biocompatibility of endodontic sealers.I Endod J.2003;36(8):527-32

9.Zmener O.Tissue response to a new methacrylate –based root canal sealer:preliminary observations in the subcutaneous connective tissue of rats

J Endod 2004; 30(5):348-351

10.Olsen Kris, Meter Austin,Hameet Walia.Osseus reaction to implanted ZOE retrograde filling materials in the tibia of rats. J Endod 1994; 20(8); 389-394

11.Bezerra Silva,Leonardo M.,Faccioli L,Figueredo F.Inflamatory response to calcium hydroxide based root canal sealers J Endod 1997;23 (2):86-90

12.Berit Olsson,Anthony Sliwkoski,Kaare Langeland.Intraosseuous implantation for biological evaluation of endodontic materials J Endodon 1981;7(6):253-265

13.Pertot W J,Camps J, Remunset M ,Proust J P. In vivo comparison of the biocompatibility of two canal-sealers implanted into the mandibular bone of rabbits.Oral Surg,Oral Med;Oral Pathol ,1992;73(5):613-20

14.Jacob Saidon,Jianing He,Qiang Zhu,Kamram Safari, Lanz Spangberg.Cell and tissue ractions to mineral trioxide agrégate and Pórtland cement.Oral Surg.Oral Med. Oral Pathol. 2003; 29(4):483-489.

15. Torabinejad M,Pitt Ford T,Alberdi Hamid and colab.Histologic asseement of mineral trioxide agrégate as a root –end filling in monkeys.J Endod 1997;23(4):225-228

16.Torabinejad M,Pitt Ford,Hamid R,Hong-Ming Tang.Tissue  reaction to implanted root-end filling materials in the tibia and mandible of guinea pigs.J Endod

1998;24 (7):468-471

17.Tagger M,Tagger E,1986 Subcutaneous  reactions to implantation of tubes with AH26 and Grossman sealer.Oral Surg. Oral Med. Oral Pathol.62 ($):434-40

18.Recommenden Standard Practices.Federation Dentaire Internacional,Comisión on dental Materials,Instruments,Equipment and Therapeutics.(1978)vol 30:185-8